## Slide 1: Test of mini-pad silicon sensor for PHENIX MPC-EX
Dahee Kim
(Ewha womans university)
for MPC-EX collaboration
Notes: ----- Meeting Notes (2/22/12 00:39) -----

## Slide 2: Contents
We report test results of prototype silicon sensors for PHENIX MPC-EX. We describe basic theory and suggest key tests for silicon sensor.
Suggested and reported key tests are
  CV characteristics
  IV characteristics
  & Electric circuitry test
Notes: 이렇게 순차적으로 test를 진행한 이유는 CV를 측정하여 full depletion이 생성되는 voltage를 찾은후 full depletion이 생성되는 구간에서 break down이 일어나지 않는지를 확인하는 IV test를 진행해야 합니다. 이러한 실험을 하던 중 channel간 문제가 발생하여 short를 확인하는 test를마지막으로 테스트를 진행하였습니다.

## Slide 3: Basic theory
Operation of PIN sensor.
Electron-hole generation & depletion region.
Notes: Silicon 빛 3.6eV정도을 흡수하면 전자 홀쌍(electron hole pari)을 생성해내~
Drift
과도핑된 보론 십의 십구승 퍼 퍼 큐빅센티미터 엔타입은 십의 십이승 십의 칠승만큼 끌어와야함 디플리션이 쉽게 됨 어시메트릭 도핑
Built-in

## Slide 4: Capacitance
Relation to depletion thickness.
17.0pF
Full
depletion region is about 23.5pF
Notes: 결론 : depletion thickness가 예상대로 형성되고 있다. Guard Ring 포함 면적보다 조금 더 deletion이 형성된다.(>>) 10%차이
Fully Depletion voltage도 강조할것 중요해!!!

## Slide 5: Simulation about CV characteristic

## Slide 6: Capacitance
(V)
bias
V
0
20
40
60
80
100
120
140
160
180
)
-
2
(
F
2
1
/
C
0
2000
4000
6000
8000
10000
18
10
´
-2
F
-1
V
19
= 5.09 x 10
2
A
Î
m
r
2
F
u
l
l
d
e
p
l
e
t
i
o
n
v
o
l
t
a
g
e

## Slide 7
Scaling with area on test pattern.
)
2
m
m
Area(
2
10
3
10
4
10
C
(
F
)
-
1
1
10
-10
10
-9
10
S
c
a
l
i
n
g
w
i
t
h
a
r
e
a
o
n
Y
S
0
2
t
e
s
t
p
a
t
t
e
r
n
.
Notes: ( 공식설명 A에 대한 정의( Guardring 포함) )
원점을 지남

## Slide 8: Current
Shockley diode equation(Ideal case)
  Simplifying idealization (drift, diffusion, thermal recombination- generation).
  Not considered : Surface leakage current, high injection, defect etc.
  With high injection(large I ),
at 300K
Notes: 에타가 1이라는 것은 ideality factor 라는 것이다.
V가 0.1볼트만 되도 -1 무시할수있을만큼 작다

## Slide 9: Forward bias current
(V)
bias
V
0.2
0.4
0.6
I
(
A
)
-7
10
-6
10
-5
10
-4
10
-3
10
-2
10
Y
S
1
1
t
e
s
t
p
a
t
t
e
r
n
,
F
o
r
w
a
r
d
-
b
i
a
s
c
h
a
r
a
c
t
e
r
i
s
t
i
c
s
T
V
V
e
0
I=I
T
2V
V
e
0
I=I
Ideal region
High injection region
S
e
r
i
e
s
r
e
s
i
s
t
a
n
c
e
d
o
m
i
n
a
t
e
d
Notes: Ideality factor
surface leakage current(가 무시할만큼 작기때문에 이 경우가 맞다.-
System 에서 갖고있는 resistance가 18옴보다 작다

## Slide 10
(V)
bias
V
0.2
0.4
0.6
I
(
A
)
0
0.002
0.004
0.006
0.008
Y
S
1
1
t
e
s
t
p
a
t
t
e
r
n
,
F
o
r
w
a
r
d
-
b
i
a
s
c
h
a
r
a
c
t
e
r
i
s
t
i
c
s
< 18
eff
R
W
0.6 (V)
»
bias
@ V

## Slide 11: Reverse bias current(Leakage current)
Source of leakage current
  Volume term
    Thermal recombination-generation leakage current
    Defect
  Surface leakage current
  Radiation(include light and cosmic ray etc..)
Notes: Leakage current가 생기는 원인은 여러가지가 있을 수 있습니다. 첫째로 volume에서 생성되는 leakage current와 (온도가 높아지면서 3.6V이상의 에너지를 받아 전류가 흐르게 됨), Defect가 존재하여 많은양의 carrier를 포함하고 있을 수 있습니다. Surface leakage current도 여러가지 이유로 생성될 수 있는데 그중 하나로 예상 되는 것은 Guard Ring부분까지 depletion이 일어나는 경우입니다.

## Slide 12: Guard ring structure
PADs of Sensor
Bonding PADs
Bias Guardring
Floating Guardring
(3 layer structure)
Edge Rounding

## Slide 13: Effect of Bias Guard Ring
YS04_L real sensor
Notes: 이경우는 defect가 적어서 Guard Ring에 bias를 주었을 때 (depletion이 빨리 일어나 가드링에 영향을 미치게되면 포텐셜 차이가 생겨서 그 사이에서 전류가 흐르게됨) surface leakage current라고 예측되는 current의 양이 작아짐을 알 수 있습니다.

## Slide 14: Effect of Dicing
Before dicing
Floating Guard Ring
YS09_L real sensor
After dicing
Notes: 5000옴이 미니멈(최소치)이다. 퓨어 실리콘을 만들고 싶은데 만들수 없기때문에 최소값을 준다. 도핑 수준은 이것의 1/3 정도이다. 더 커질수도 있다!!!
Surface leakage current가 주요 원인이다.

## Slide 15: Electric circuit test
We measured resistance between neighboring channels. Small fraction of them had short. Current yield ~ 30%. Statistics suggest the short is between metal traces. Stringent metal etching process is expected to cure the problem.
30 
30 
1.5 cm
1.5 cm
3 cm
1
2
3
4
Cut line
6 cm
Electric short happens between neighboring channels.
The short frequency is proportional to trace overlap.
Notes: 센서에 배선이 제대로 됐는지를 확인하는 과정에서 쇼트가 된것을 확인하였다.
그러한 비율로 쇼트가 일어날것이라고 생각하고 테스트하고 있다. 128 채널중에 한두개

## Slide 16: Summary
We measured full depletion voltage for 425μm wafer to be 35V which corresponds to resistivity ~15,000 Ωcm.
No breakdown is observed until the reverse bias voltage of 250V.
We observed low leakage current less than 1μA for the whole sensor of 6 x 6 cm.
We identified a small number of shorts between neighboring channels and attribute the problem to close metal traces. We propose further etching process for metal layer and/or increased space between metal traces.